ID Card for FeSi

Registration of FeSi As multi-constituent substance.

Date: April 2010

Material identification of parameters for REACH

| 2. | IDENTIFICATION OF THE MATERIAL: Ferrosilicon alloys |
| --- | --- |
| 2.1 | Name or other identifier of each preparation |
| 2.1.1 | Name(s) in the IUPAC nomenclature or other international chemical name(s) Ferro-silicon alloy, iron-silicon alloy, ferrosilicon alloy, iron silicide alloy, iron disilicide alloy, Reaction mass of iron and iron disilicide and iron silicide and silicon |
| 2.1.2 | Other names (usual name, trade name, abbreviation) As 2.1.1, master alloys, inoculants (smelting) |
| 2.1.3 | EINECS or ELINCS numbers (if available and appropriate) 234-670-2/234-671-8/--- As reaction mass (see above): 912-631-7 |
| 2.1.4 | CAS name and CAS numbers (if available) 12022-95-6 /12022-99-0/8049-17-0 --- |
| 2.1.5 | Other identity codes (if available): ISO or other standards ISO 5445 ferrosilicon alloys |
| 2.2 | Information related to molecular and structural formula of each preparation |
| 2.2.1 | Molecular and structural formula (including SMILES notation, if available) n.a. See enclosed phase diagram FeSi, FeSi2 (FeSi2,l, FeSi2,h), Si For nodularisers and inoculants there will be additional phases, according to other elements present |
| 2.2.2 | Physical form(s) or particle distributions Lumpy, granular, ingot, sieving sizes, atomized, milled Reference to a typical size distribution |
| 2.2.3 | Molecular weight or molecular weight range/atomic weight range/weight % range of Fe and Si Typical commercial weight range Si: 8 – 95.1, other metals range 0 – 12, Fe 4 – 88 |
| 2.3 | Composition 1 |
| 2.3.1 | Weight % of all constituents, major, minor and trace elements See Annex |
| 2.3.2 | Chemical nature of constituents See Annex |
| 2.3.3 | Weight percentage and nature of impurities See Annex |
| 2.3.4 | Chemical nature and order of magnitude (…ppm, ….%) of any additives intentionally added (i.e., minor elements) |
| 2.3.5 | Spectral data (ultra-violet, infra-red, nuclear magnetic resonance or mass spectrum) Inorganic material, thus irrelevant. |
| 2.3.7 | Description of the analytical methods or the appropriate bibliographical references for the identification of each substance/ constituent and, where appropriate, for the identification of impurities and additives. This information shall be sufficient to allow the methods to be reproduced. ISO 5445 – Methods: 4139 – 4158 The Si is precipitated like Potassium Hexafluorsilicate and analyzed by titrimetric method with sodium hydroxide. Others metallic impurities are analyzed by ICP - Inductively coupled plasma Carbon and sulphur analyzed by infra red (JIS G 1312) Acid digestion + ICP XRF calibrated to international standards. |
| 2.4 | Production process |
|  | Ferrosilicon is produced in low-shaft three phase submerged electric arc furnaces, using the Søderberg-technology, by reducing oxides like quartz, iron oxides or iron chips with carbon from coke, coal, charcoal, pet. coke, wood chips, and alloying elements as iron, etc. |
| 2.5 | State known use(s) of each of the ferrosilicon qualities mentioned above: The typical applications are: Deoxidation and alloying of steel melts Alloying of cast iron charges and melts (Iron foundries) Silicothermic reduction of precious metals (Cr, V, Mo) and others (Nb, W). Production of some inoculants and nodulisers by alloying (melting) Other applications are: High purity FeSi is used to produce high permeability steel for electric transformers. Production of FeSiMn, FeSiN and SiMn- alloys. FeSi 15% is used for metal separation by dense-media process and production of welding products. It is also used as metal filler. |

| 2.3. Composition of FeSi alloys (45, 65, 75, 90 % Si, inoculants & noduliers) 15 % |
| --- |
| Name of the Constituent | Chemical formula | Oxidation number | Value | Name of analytic method | Actual detection level | Reference |
|  |  |  | Range in % | geometric mean | arithmetic mean | RSD |  |  |  |
| Major constituent |  |  |  |  |  |  |  |  |  |
| Silicon | Si | Met | 8 – 95.1 |  |  |  | XRF |  | ISO 5445 |
| Major Element |  |  |  |  |  |  |  |  |  |
| Iron |  |  | 4 - 88 |  |  |  | XRF |  |  |
| Other elements |  |  |  |  |  |  |  |  |  |
| Aluminium | Al | Met | 0 – 6 |  |  |  | XRF |  |  |
| Calcium | Ca | CaSi | 0 - 5 |  |  |  | XRF |  |  |
| Zirconium | Zr | Met | 0 – 8 |  |  |  | XRF |  |  |
| Manganese | Mn |  | 0 – < 1 |  |  |  | XRF |  |  |
| Magnesium | Mg |  | 0 – < 0.1 |  |  |  | XRF |  |  |
| Barium | Ba |  | 0 – 12 |  |  |  | XRF |  |  |
| Strontium | Sr |  | 0 – 1.5 |  |  |  | XRF |  |  |
| Cerium | Ce |  | 0 - < 0.1 |  |  |  | XRF |  |  |
| Lanthanum | La |  | 0 – < 0.1 |  |  |  | XRF |  |  |
| Praseodynium | Pr |  | 0 – < 0.1 |  |  |  | XRF |  |  |
| Neodynium | Nd |  | 0 – < 0.1 |  |  |  | XRF |  |  |
| Yttrium | Y |  | 0 – < 0.1 |  |  |  | XRF |  |  |
| Sulfur | S |  | 0 – 2.5 |  |  |  | XRF |  |  |
| Bismuth | Bi |  | 0 – 1.3 |  |  |  | XRF |  |  |
| Tin | Sn |  | 0 – 1 |  |  |  | XRF |  |  |
| Titanium | Ti |  | 0 – 11 |  |  |  | XRF |  |  |
| Trace elements - Impurities |  |  |  |  |  |  |  |  |  |
| Phosporus | P |  | 0 – 0. 15 |  |  |  | XRF |  |  |
| Carbon | C |  | 0 – 1.35 |  |  |  | XRF |  |  |
| Chromium | Cr |  | 0 – 0.5 |  |  |  | XRF |  |  |
| Boron | B |  | < 0.009 |  |  |  | XRF |  |  |
| Copper | Cu |  | 0 – 0.2 |  |  |  | XRF |  |  |
| Cadmium | Cd |  | 0 – < 0.1 |  |  |  | XRF |  |  |
| Arsenic | As |  | 0 – < 0.1 |  |  |  | XRF |  |  |
| Nickel | Ni |  | 0 – < 0.1 |  |  |  | XRF |  |  |
| Lead | Pb |  | 0 – 0.01 |  |  |  | XRF |  |  |
| Zinc | Zn |  | 0 – 1.2 |  |  |  | XRF |  |  |
| Molybdenum | Mo |  | 0 – 0.01 |  |  |  | XRF |  |  |
| Antimony | Sb |  | 0 – 0.01 |  |  |  | XRF |  |  |
| Cobalt | Co |  | 0 – 0.01 |  |  |  | XRF |  |  |
| Nitrogen | N | FeSiN | 0-0.01 |  |  |  | XRF |  |  |

FeSi phase diagram

# Footnotes

The species/mineralogical form under which a certain element or compound is present in a substance/material should be specified when possible (key parameter to discuss and agree on substance sameness and substance classification).

The species/mineralogical form under which a certain element or compound is present in a substance/material should be specified when possible (key parameter to discuss and agree on substance sameness and substance classification.

Only Si is in the elemental form