Draft ID Card for Si/FeSi silicate

Date: March 2009

Substance identification of parameters for REACH

| 2. | IDENTIFICATION OF THE SUBSTANCE: Si/FeSi silicate |
| --- | --- |
| 2.1 | Name or other identifier of the substance |
| 2.1.1 | Name(s) in the IUPAC nomenclature or other international chemical name(s) Slags, elec. furnace smelting, iron silicate (EINECS) |
| 2.1.2 | Other names (usual name, trade name, abbreviation) Si/FeSi Silicate Si/FeSi secondary product Aluminium silicate, Calcium silicate, Magnesium silicate, Silicon carbide |
| 2.1.3 | EINECS or ELINCS numbers (if available and appropriate) 310-060-2 |
| 2.1.4 | CAS name and CAS numbers (if available) 102110-59-8 |
| 2.1.5 | Other identity codes (if available): ISO or other standards --- |
| 2.2 | Information related to molecular and structural formula of the substance |
| 2.2.1 | Molecular and structural formula (including SMILES notation, if available) See 2.3.1 |
| 2.2.2 | Physical form(s) or particle distributions Lumpy, granular |
| 2.2.3 | Molecular weight or molecular weight range/atomic weight range/weight % range See 2.3.1 |
| 2.3 | Composition of the substance |
| 2.3.1 | Weight % of all constituents, major, minor and trace elements Degree of purity (%) Constituent Formula EC# CAS# Weight% Aluminium silicate Al2SiO5 235-253-8 12141-46-7 25 – 75% Calcium silicate CaSiO3 233-250-6 10101-39-0 25 – 75% Magnesium silicate MgSiO3 237-413-2 13776-74-4 0 – 50% Silicon carbide SiC 206-991-8 409-21-2 0 – 25% |
| 2.3.2 | Content of impurities N/A if registered as UVCB |
| 2.3.3 | Weight percentage and nature of impurities N/A |
| 2.3.4 | Chemical nature and order of magnitude (…ppm, ….%) of any additives intentionally added N/A |
| 2.3.5 | Spectral data (ultra-violet, infra-red, nuclear magnetic resonance or mass spectrum) Inorganic material ,thus irrelevant. |
| 2.3.7 | Description of the analytical methods or the appropriate bibliographical references for the identification of each substance/ constituent and, where appropriate, for the identification of impurities and additives. This information shall be sufficient to allow the methods to be reproduced. ICP - Inductively coupled plasma Acid digestion + ICP XRF calibrated to international standards. |
| 2.4 | Production process |
|  | Smelting process in an electric arc furnace or ladle treatment. Typical raw materials are: Elemental carbon like coal, charcoal, woodchips, petcoke, consumable electrodes SiO2 like quartz, sand, others iron oxides, limestone |
| 2.5 | State known use(s) of the substance For the production of silicomanganese, slag formation in steel, briquettes, etc. |

# Footnotes

The species/mineralogical form under which a certain element or compound is present in a substance/material should be specified when possible (key parameter to discuss and agree on substance sameness and substance classification).